Guangzhou Guanzhi New Material Technology Co., Ltd.

Tel: +86 20 8256 7990	Fax: +86 20 3221 4789

Address: Room 1106, Block A, Guangzhou International Business Incubator, No. 3 Juquan Road, Science City, Huangpu District, Guangzhou, China

Waterborne Epoxy Dispersion EP-1704

【Characterization】

EP-1704 is a waterborne dispersion of E20 epoxy resin, particularly suitable for waterborne metal anti-corrosion primers.

【Specification Property】

| Item | Index | Unit | Test method |
| --- | --- | --- | --- |
| Emulsion appearance | Milky white liquid |  | Visual inspection |
| Epoxy equivalent weight (EEW) | 900-1100 | g/mol |  |
| Solid content | 53±2 | % | 150 °C for 30 min, convection oven |
| pH value (25 °C) | 6.0-8.0 |  | GB/T 6920-1986 |
| Viscosity (25 °C) | 200-5000 | mPa·s | GB/T 2794-2013 |

【Product Features】

- Self-emulsifying solid epoxy with excellent storage stability and consistent viscosity during storage;

- High tolerance for formulation design and suitable for direct use in color paste grinding.

【Application】

EP-1704 provides excellent adhesion to most metal substrates and is suitable for anti-corrosion primers and protective coatings. For improved corrosion resistance, the recommended curing-agent dosage is 85±5% of the chemically calculated theoretical amount.

【Storage】

EP-1704 waterborne epoxy dispersion must be stored in a sealed container. Store at 5-35 °C and protect from freezing. Do not mix with paints. The shelf life is 6 months from the date of shipment; product performance should be evaluated before use to ensure safe application.